Investigation of fracture initiation angle and propagation path for PUR foams under mixed mode I/III loading

Mohammad Reza Mohammad Aliha (MRM. Aliha)

Welding and Joining Research Center, Iran University of Science and Technology (IUST), Narmak, 16846-13114, Tehran, Iran.

mrm_aliha@iust.ac.ir (Corresponding Author)

Aram Bahmani (A. Bahmani)

Department of Mechanical and Mechatronics Engineering, University of Waterloo, 200 University Avenue West, Waterloo, ON N2L 3G1, Canada

Email: bahmaniaram@yahoo.com

Emanoil Linul (E. Linul)

Department of Mechanics and Strength of Materials, Politehnica University of Timisoara, Blvd. M.. Viteazu, No. 1, Timisoara 300222, Romania

Email: emanoil.linul@upt.ro

Top of Form

Bottom of Form

Liviu Marsavina (L. Marsavina)

Department of Mechanics and Strength of Materials, Politehnica University of Timisoara, Blvd. M.. Viteazu, No. 1, Timisoara 300222, Romania

Email: liviu.marsavina@upt.ro

Sina Samareh Mousavi (SS. Mousavi)

Welding and Joining Research Center, Iran University of Science and Technology (IUST), Narmak, 16846-13114, Tehran, Iran.

s_samareh@mecheng.iust.ac.ir

Atefeh Mousavi (A. Mousavi)

Welding and Joining Research Center, Iran University of Science and Technology (IUST), Narmak, 16846-13114, Tehran, Iran.

moosavi.atefe@yahoo.com

Abstract. Mixed mode I/III (i.e. tensile-tear) fracture is one of the possible failure modes in engineering components and structures subjected to out-of plane loads and deformations. Under such loading conditions fracture direction is twisted from the initial crack plane. Study of fracture initiation direction and propagation path under mixed mode I/III is therefore of practical interest for fracture mechanics researchers and engineers. Recently, the authors have proposed a novel and new test specimen called “edge notched disc bend- ENDB” for conducting mixed mode I/III fracture experiments. In this paper, the practical ability of this specimen was examined for fracture and crack growth testing of a medium density rigid PUR foam material under mixed mode I/III loading. It was observed that the mixed mode I/III fracture path grows along a curvilinear out-of plane trajectory that exhibits an anti-symmetric fracture plane relative to the mid-section of ENDB specimen. The direction of initial fracture along the entire crack front in the tested ENDB specimens made of PUR foam was predicted numerically for different mode mixities and it was shown that these predictions (that are based on the maximum tangential stress criterion) are in good agreement with the obtained experimental data. Keywords. Mixed mode I/III, Rigid PUR foam, fracture initiation angle, Edge notched disc bend configuration.

Introduction

Rigid polymeric foams such as Polyurethane (PUR) foams are now frequently used in many industrial applications due to their good mechanical and physical properties like high insulation, low-density, high porosity, lightweight structure and good energy absorption capacity. The mechanical properties of such foams are influenced by: (i) the mechanical properties of polymer and ceramics materials which the foam is made, (ii) the topology and shape of cellular structure (open cell, closed cell or mixed closed-open cells) and (iii) the densities of cellular and solid materials. Crack growth and brittle fracture is a major weakness for rigid foam components [1,2]. Mode III or out-of-plane sliding of crack flanks (that is usually occurs due to the application of torsional type loads) is possible mode of fracture growth in cracked components. For example, the sandwich panel structures with foam cores may experience a complex combination of bending moments and torsional couples, simultaneously. In such loading conditions, a mixed mode tensile-tear (i.e. mixed mode I/III) fracture mechanism can govern the overall failure behavior of foam cores used in the structure of sandwich panels. It is well understood that under the influence of out-of-plane sliding deformation applied to the crack flanks in a specimen, the trajectory of fracture tends to grow in a non-coplanar path along a twisted direction with respect to the crack plane. Several studies have been done in the past to investigate the crack propagation behavior under tensile-tear loading using different test specimens. Example of these specimens include single-edge notch beam [3], edge cracked plate loaded by pin loading [4], circumferentially notched bar [5, 6] and edge notched disc bend (ENDB) specimen [7]. Some fracture characteristics including the load bearing capacity, direction and path of fracture growth are usually investigated and obtained experimentally using these test geometries. A few analytical models and fracture theories such as maximum tangential strain energy density (MTSED) [8], and maximum tangential stress (MTS) [9] were also proposed to predict the crack initiation angle under mixed mode loading condition. Although the reported studies have made many contributions in this field, assessment of crack path subjected to the mixed mode I/III has not been explored experimentally and numerically for rigid foam materials. In this study, the crack initiation angle of polyurethane (PUR) foam is investigated by employing the edge notched disc bend (ENDB) specimen. Some mixed mode I/III fracture experiments are conducted on the ENDB specimen at different mode mixities and the variations of fracture initiation angle thorough the crack front is determined experimentally. It is shown that the obtained experimental results are in good agreement with the predictions of the MTS criterion.

Fracture Experiments

Fig. 1 represents the geometry and loading configuration of the ENDB specimen (used for foam fracture testing) with radius R and thickness B that contains an edge crack of depth a created through the disc diameter. The ENDB is loaded by a simple and conventional three-point bend fixture with bottom loading span of 2S. The crack plane makes an inclination angle of β relative to the loading rollers (or the vertical direction). By changing the crack angle β, the state of crack flank deformation varies from pure mode I (opening of crack flanks) for β =0° to mixed mode I/III (combined opening and out-of plane sliding of crack flanks). PUR foam with closed-cell microstructure and density of 145 kg/m3, manufactured by NECUMER GmbH-Germany, was used to prepare the ENDB specimens for mixed mode I/III fracture tests. Overall dimensions of the prepared ENDB specimens for fracture experiments were as follows: R= 75 mm, B = 30 mm and a = 15 mm. For covering the full modes I and III mixities, the following crack inclination angles computed numerically via finite element analyses [8] of ENDB in the ABAQUS code,  were considered {β=0° (pure mode I), 45, and 64° (pure mode III)}. The loading span for all test specimens was fixed and constant equal to 69 mm. The specimens were loaded with constant cross head speed of 2 mm/min until the final fracture using a Zwick Proline Z005 testing machine.

Fig.1. Geometry, loading configuration and dimensions of the ENDB specimen.

The state of mode mixity and the contribution of modes I and III in this specimen are function of a, 2S, and β.

Accordingly, the geometry factors (YI and YIII) for the ENDB specimen can be determined from [10-13]:

|  | (1) |
| --- | --- |
|  | (2) |

where P is the distributed load applied by the upper loading roller, while KI and KIII are the stress intensity factors for mode I and mode III, respectively. At the onset of fracture, which is expected to start from the mid-section [13], the ENDB specimen experiences a certain combination of mixed mode I/III depending on a, 2S and β. By increasing β from zero, KI value decreases and conversely the contribution of mode III component (KIII) increases. Variations of geometry factors (YI and YIII) for different geometries and loading conditions of the investigated ENDB specimen have been presented in Fig. 2. This Figure shows that the ENDB specimen can cover full range of mode mixities from pure mode I to pure mode III when β varies from zero to approximately 65°. Accordingly, some ENDB specimens made of PUR foams were manufactured from PUR foam with density of 145 kg/m3. The ENDB specimens were then loaded monotonically using a three-point bend fixture with loading rate of 1 mm/min up to the final fracture. Fig. 3 shows the ENDB loading test setup for pure mode I and mixed mode I/III.

Fig.2. Variations of mixed modes I and III geometry factors in the mid-section of ENDB specimen for different crack orientation angles (β).

Results and discussion

The fracture toughness values of tested foams were as follows: KIc = 3.56 MPa.mm0.5, KI/III = 3.31 MPa.mm0.5 and KIIIc = 2.90 MPa.mm0.5 that reveals the crack growth resistance of PUR foam in tensile failure is greater than the anti-symmetric tear type fracture (i.e. mode III). Fig. 4 shows also the fracture trajectories of fractured PUR foams under different loading modes. As seen from this Figure, the fracture initiation angle and consequently the path of fracture differ for different crack front locations and mode mixities.  While mode I fracture path is self-similar and along the direction of initial crack plane, mixed mode I/III and pure mode III fracture trajectory twists from the crack plane. I addition while fracture initiation angle (θ0) is zero exactly at the mid-section (z/R=0) of ENDB specimen, by increasing the z/R and moving towards the corner points, the corresponding value of θ0 becomes greater. This difference in the value of θ0 for different z/R values of ENDB specimen results in a twisted trajectory for mode III and mixed mode I/III specimen.

| (a) | (b) |
| --- | --- |

Fig.3. Test setup for ENDB testing of PUR foams (a) pure mode I and (b) mixed mode I/III loading conditions.

| (a) | (b) | (c) |
| --- | --- | --- |

Fig.4. Fracture path observed for ENDB specimens under (a) pure mode I, (b) mixed mode I/III and (c) pure mode III conditions.

For determining the fracture initiation angles the specimens were cut perpendicular to the crack front location at five z/R values of 0, 0.25, 0.5, 0.75, and 1. The corresponding fracture initiation values (θ0) were measured using digitized images of cross –sections in a KRUSS microscope as shown schematically for one of the ENDB specimens in Fig. 5. The fracture initiation angles measured experimentally at different z/R values ranging from -1 to 1 have been presented in Fig. 6. From the other hand, the direction of fracture initiation angle for any desired location (z/R) of ENDB specimen can be computed and predicted using available fracture models. For example, in this research, we determined the variations of θ0 versus z/R for different modes I and III mixities of investigated ENDB specimens made of PUR foam. The maximum tangential stress (MTS) criterion [8] that has been built in the ABAQUS finite element software [14] was utilized for obtaining θ0 value. First a FE model of ENDB specimen was created in the ABAQUS code with exactly the same dimensions, geometry, and loading supports of the tested ENDB specimen (i.e., a/B = 0.5, S/R = 0.92, and β = 0, 45, 64°) and then by preparing a static analysis the direction of fracture initiation angle θ0 was determined via the MTS criterion through the entire crack front. Fig. 6 shows the computed θ0 values for different z/R values of ENDB specimen and different mode mixities (or crack inclination angles). This figure also compares the experimental crack initiation angles with the predicted θ0 values for the investigated ENDB specimen made of PUR foam. An excellent agreement is seen between the experimental data and theoretical (or numerical) estimations.

Fig.5. Fracture initiation measurement for the tip of crack in the broken foam specimen made of ENDB specimen.

Fig.6. Comparison of fracture initiation angle for different crack inclination angles (β) along the crack front obtained from experiments and predictions of MTS criterion.

Conclusions

- Mixed mode I/III fracture of medium density PUR foam was investigated experimentally using the ENDB specimen. The fracture toughness of tested material was reduced by moving from pure mode I towards pure mode III.

- A twisted fracture trajectory was observed for the tested foams under mixed mode I/III loading condition and by increasing the contribution of mode III component, the fracture path showed more deviation from the pre-crack plane.

- The direction of fracture initiation angle was measured for the tested foam along the crack front and it was shown that the obtained mixed mode I/III fracture angles can be predicted very well with the maximum tangential stress criterion.

References

[1] Marsavina L., Linul E., Voiconi T., Sadowski T. A comparison between dynamic and static fracture toughness of polyurethane foams, Polymer Testing., (2013), 32, 673-680.

[2] Negru R., Marsavina L., Voiconi T., E Linul., Filipescu H., Belgiu G., Application of TCD for brittle fracture of notched PUR materials, Theoretical and Applied Fracture Mechanics 80 (2015)  87-95.

[3] Ahmadi-Moghadam, B., & Taheri, F., An effective means for evaluating mixed-mode I/III stress intensity factors using single-edge notch beam specimen, J. Strain. Analysis. Eng. Des., (2013), 48, 245-257.

[4] Ayatollahi, M. R., & Saboori, B., A new fixture for fracture tests under mixed mode I/III loading, Europ. J. Mech. A/Solids., (2015), 51, 67-76.

[5] Berto, F., Cendon, D. A., Lazzarin, P., & Elices, M., Fracture behaviour of notched round bars made of PMMA subjected to torsion at− 60 C, Eng. Fract. Mech., (2013), 102, 271-287.

[6] Berto, F., Elices, M., Lazzarin, P., & Zappalorto, M., Fracture behaviour of notched round bars made of PMMA subjected to torsion at room temperature, Eng. Fract. Mech., (2012), 90, 143-160.

[7] Ayatollahi, M. R., & Saboori, B., Maximum tangential strain energy density criterion for general mixed mode I/II/III brittle fracture. Int. J. Damage. Mech., (2015), 24, 263-278.

[8] Liu, S., Chao, Y. J., & Zhu, X., Tensile-shear transition in mixed mode I/III fracture, Int. J. Solids. Struct., (2004), 41, 6147-6172.

[9] Aliha, M. R. M., Linul, E., Bahmani, A., & Marsavina, L., Experimental and theoretical fracture toughness investigation of PUR foams under mixed mode I+ III loading, (2018), Polymer. Test., 67, 75-83.

[10] Aliha, M. R. M., & Bahmani, A., Rock fracture toughness study under mixed mode I/III loading, Rock Mech. Rock. Eng., (2017), 50, 1739-1751.

[11] Aliha, M. R. M., Sarbijan, M. J., & Bahmani, A., Fracture toughness determination of modified HMA mixtures with two novel disc shape configurations. Construct. Build. Mater., (2017), 155, 789-799.

[12] Bahmani, A., Aliha, M. R. M., & Berto, F., Investigation of fracture toughness for a polycrystalline graphite under combined tensile-tear deformation. Theor. Applied. Fract. Mech., (2017), 90, 53-64.

[13] Aliha, M. R. M., Bahmani, A., & Akhondi, S., Numerical analysis of a new mixed mode I/III fracture test specimen, Eng. Fract. Mech., (2015), 134, 95-110.

[14] Simulia, D., Analysis User Manual. Abaqus/Standard 2014.